## Slide 1: Nucleation sites of preciptates in MatCalc simulations (MatCalc 5.61.0017)
P. Warczok

## Slide 2: What is it all about?

## Slide 3: What is it all about?
Consequences
  Number of available nucleation sites
  Interfacial energy model
  Precipitate growth & coarsening  nucleation on grain boundaries
  Special cases: Nucleation on/within precipitates

## Slide 4: Number of available nucleation sites
  Nucleation rate 
  Available nucleation sites – bulk
  Available nucleation sites – dislocations
  Nbulk
  Ndisl
– Nucleation rate
– Number of nucleation sites
on position
– Avogadro number
– Molar volume
– Dislocation density

## Slide 5: Number of available nucleation sites
  Grain&subgrain boundaries – tetra(kai)decahedron concept
    Strictly: Truncated octahedron
a
– Volume of the polygon
– Total surface of the polygon
– Total edge length of the polygon
http://mathworld.wolfram.com/TruncatedOctahedron.html

## Slide 6: Number of available nucleation sites
  Grain&subgrain boundaries – tetra(kai)decahedron concept
    Strictly: Truncated octahedron
– Volume of the polygon
– Total surface of the polygon
– Total edge length of the polygon
– Grain diameter
– Subgrain diameter

## Slide 7: Number of available nucleation sites
  Grain&subgrain boundaries – tetra(kai)decahedron concept
    Strictly: Truncated octahedron
– Volume of the polygon
– Total surface of the polygon
– Total edge length of the polygon
– Grain diameter
– Subgrain diameter
– Elongation factor for grains
– Elongation factor for subgrains

## Slide 8: Number of available nucleation sites
  Grain&subgrain boundaries – tetra(kai)decahedron concept
    Strictly: Truncated octahedron
– Grain diameter
– Subgrain diameter
– Elongation factor for grains
– Elongation factor for subgrains

## Slide 9: Number of available nucleation sites
  Available nucleation sites – grain&subgrain boundaries
  Available nucleation sites – grain&subgrain boundary edges
  Available nucleation sites – grain&subgrain boundary corners

## Slide 10: Number of available nucleation sites
„Nucleation site efficiency“ scales linearly the number of available nucleation sites

## Slide 11: Interfacial energy model
  Bulk & dislocations  standard interfacial energy evaluation
  Grain & subgrains (surface, edges, corners)  Clemm-Fisher model
– Grain boundary energy
– Precipitate/matrix interfacial energy
Clemm P.J., Fisher J.C., Acta Metall. 3 (1955) 70-73

## Slide 12: Interfacial energy model
  Bulk & dislocations  standard interfacial energy evaluation
  Grain & subgrains (surface, edges, corners)  Clemm-Fisher model
– Grain boundary energy
– Precipitate/matrix interfacial energy

## Slide 13: Interfacial energy model
  Grain & subgrains surfaces
Clemm P.J., Fisher J.C., Acta Metall. 3 (1955) 70-73

## Slide 14: Interfacial energy model
  Grain & subgrains edges
Clemm P.J., Fisher J.C., Acta Metall. 3 (1955) 70-73

## Slide 15: Interfacial energy model
  Grain & subgrains corners
Clemm P.J., Fisher J.C., Acta Metall. 3 (1955) 70-73

## Slide 16: Interfacial energy model
  Clemm-Fisher model needs to be activated!
Clemm P.J., Fisher J.C., Acta Metall. 3 (1955) 70-73

## Slide 17: Interfacial energy model
  Bulk & dislocations  standard interfacial energy evaluation
  Grain & subgrains (surface, edges, corners)  Clemm-Fisher model
– Grain boundary energy
– Precipitate/matrix interfacial energy
Clemm P.J., Fisher J.C., Acta Metall. 3 (1955) 70-73

## Slide 18: Precipitate growth & coarsening
  Difference in diffusion fields

## Slide 19: Precipitate growth & coarsening
  Difference in diffusion fields  modification of radius evolution equations derived from thermodynamic extremum principle
Kozeschnik et al., Modelling Simul. Mater. Sci. Eng. 18 (2010) 015011

## Slide 20: Precipitate growth & coarsening
  Difference in diffusion fields  modification of radius evolution equations derived from thermodynamic extremum principle
Kozeschnik et al., Modelling Simul. Mater. Sci. Eng. 18 (2010) 015011
Precipitation of AlN at austenite at grain boundaries

## Slide 21: Precipitate growth & coarsening
  Difference in diffusion fields  modification of radius evolution equations derived from thermodynamic extremum principle
Kozeschnik et al., Modelling Simul. Mater. Sci. Eng. 18 (2010) 015011
Precipitation of AlN at austenite at grain boundaries
NOTE:
The grain boundary diffusion field model is automatically used when “grain boundary” is selected as the nucleation site
This model is relevant for the system with large grain size and small precipitate phase fractions.
In other cases, use the random diffusion field model  select other nucleation sites (e.g. “dislocations”) and adjust the available number of the nucleation sites using the “nucleation site efficiency”

## Slide 22: Nucleation on the precipitate surface

## Slide 23: Nucleation on the precipitate surface
  Available nucleation sites  atoms on the surface of the parent phase
  Parent phase is not modified by the nucleation of the new phase
- Number of precipitates in class „j“
- Radius of precipitates in class „j“

## Slide 24: Nucleation within the precipitate

## Slide 25: Nucleation within the precipitate
  Available nucleation sites  atoms on the surface of the parent phase (as in the previous case)
  Nucleation  ,
  Interfacial energy defined by user, critical radius from parent prec.
  Parent phase transforms gradually into the new one
- Driving force of the new phase
- Driving force of the parent phase
- Nucleation driving force of the new phase

## Slide 26: Transformation of the precipitate

## Slide 27: Transformation of the precipitate
  „Transformation towards“ rather than „nucleation of“ the new precipitate
  Transformation condition: ,
  New precipitate size taken from the parent phase
  Initial precipitate composition might be taken from the parent phase

## Slide 28: Transformation of the precipitate
  Parent phase transforms gradually into the new one

## Slide 29: Transformation of the precipitate
  Parent phase transforms gradually into the new one

## Slide 30: Direct particle transformation
For the two last cases:
(nucleation within and transformation of the precipitate)
Change the nucleation model to „direct particle transformation“!

## Slide 31: Acknowledgments
Yao Shan