## Slide 1: Performing Scheil-Gulliver (SG) analysis in MatCalc (MatCalc 5.62.0013)
P. Warczok

## Slide 2: Outline
Solid phase composition after alloy solidification
  Back-diffusion effect
  Primary precipitates
  Modeling of solid-solid transformation

## Slide 3: Solid phase composition after alloy solidification

## Slide 4: Solid phase composition
Experimental observation: Microsegregation in solidified phase
Pudar M. et al., Steel Res. Int. 81 (2010) 372-80

## Slide 5: Solid phase composition
Theoretical estimation: equilibrium diagram
http://www.sv.vt.edu/classes/MSE2094_NoteBook/96ClassProj/examples/cu-ni.html
(43 wt% Ni)

## Slide 6: Solid phase composition
http://www.sv.vt.edu/classes/MSE2094_NoteBook/96ClassProj/examples/cu-ni.html
Yes, if diffusion in the phases is fast enough…
Are these phase compositions real?
Diffusion in the solid phase is the limiting parameter
Theoretical estimation: equilibrium diagram

## Slide 7: Solid phase composition
Theoretical estimation: stepped solidification
CL,1
CS,1
http://matcalc.tuwien.ac.at/index.php/documentation/detail.php?id=tutorials;t11&media=tutorials;t11;img;t11_figure1v2.png

## Slide 8: Solid phase composition
Theoretical estimation: stepped solidification
CL,2
CS,2
CS,1
http://matcalc.tuwien.ac.at/index.php/documentation/detail.php?id=tutorials;t11&media=tutorials;t11;img;t11_figure1v2.png

## Slide 9: Solid phase composition
Theoretical estimation: stepped solidification
http://matcalc.tuwien.ac.at/index.php/documentation/detail.php?id=tutorials;t11&media=tutorials;t11;img;t11_figure1v2.png
CS,3
CS,2
CS,1
CL,3

## Slide 10: Solid phase composition
Theoretical estimation: Scheil equation
Liquid
Solid
L+S
Gulliver G.H., J. Inst. Met. 9 (1913) 120-54
Scheil E., Z. Metall. 34 (1942) 70-72

## Slide 11: Solid phase composition
Theoretical estimation: Scheil equation
Pro: Nice analytical solution
Contra: Formula dependent on system specification
Valid for k = const. !

## Slide 12: What MatCalc does?
http://matcalc.tuwien.ac.at/index.php/documentation/detail.php?id=tutorials;t11&media=tutorials;t11;img;t11_figure1v2.png
Liquid(CL,1)
α(CS,1)
Stepped solidification  SG-calculation

## Slide 13: What MatCalc does?
http://matcalc.tuwien.ac.at/index.php/documentation/detail.php?id=tutorials;t11&media=tutorials;t11;img;t11_figure1v2.png
Liquid(CL,1)
α(CS,1)
New equilibrium phase α with solute content CS,1 created
Liquid composition set to CL,1

## Slide 14: What MatCalc does?
http://matcalc.tuwien.ac.at/index.php/documentation/detail.php?id=tutorials;t11&media=tutorials;t11;img;t11_figure1v2.png
α(CS,2)
α_S(CS,1)
Liquid(CL,2)

## Slide 15: What MatCalc does?
α(CS,2)
α_S(CS,1)
http://matcalc.tuwien.ac.at/index.php/documentation/detail.php?id=tutorials;t11&media=tutorials;t11;img;t11_figure1v2.png
Liquid(CL,2)
Previous α-phase is denoted now α_S
α_S gets a „dormant“ status (phase fraction and composition are „frozen“)
New equilib. phase α with solute content CS,2 created
Liquid composition set to CL,2

## Slide 16: What MatCalc does?
http://matcalc.tuwien.ac.at/index.php/documentation/detail.php?id=tutorials;t11&media=tutorials;t11;img;t11_figure1v2.png
Liquid(CL,3)
α(CS,3)
α_S(Cα)

## Slide 17: What MatCalc does?
Liquid(CL,3)
α(CS,3)
α_S(Cα)
α_S formed by merging the previous α_S and previous α (adding phase fractions)
α_S composition is evaluated from mass balance of the merged phases
„Dormant“ status set to α_S
New equilib. phase α with solute content CS,3 created
Liquid composition set to CL,3

## Slide 18: What MatCalc does?
Liquid(CL,3)
α(CS,3)
α_S(Cα)
Technical note
„α“-phase contains the fraction solidified at the considered temperature
„α_S“-phase contains all fractions solidified before the considered temperature

## Slide 19: Example
Cu-Ni alloy, 35 wt.% Ni
Temperature [°C]
Temperature [°C]
Phase fraction
Phase fraction
Liquid
Liquid
FCC_A1
FCC_A1_S
FCC_A1
Equilibrium calculation
SG-calculation

## Slide 20: Example
Cu-Ni alloy, 35 wt.% Ni
Temperature [°C]
Temperature [°C]
Ni content [wt.%]
Ni content [wt.%]
Liquid
Liquid
FCC_A1
FCC_A1_S
FCC_A1
Equilibrium calculation
SG-calculation

## Slide 21: Back-diffusion effect

## Slide 22: Backdiffusion
Some elements might be permitted to equilibrate fast between the liquid and solid phases
Relevant for interstitial elements (B,C,N)  diffuse fast enough on the interstitial lattice

## Slide 23: Backdiffusion
Technical note
„_S“-phase has a „fixed phase fraction flag“ and constraints on u-fraction of elements with „no“ setting for back-diffusion (it is not „dormant“ any more)

## Slide 24: Example
Fe-Mn-C alloy, 3 wt.% Mn, 0.7 wt.% C (Tutorial 11)
Temperature [°C]
Phase fraction
Liquid
Liquid
With BD

## Slide 25: Example
Fe-Mn-C alloy, 3 wt.% Mn, 0.7 wt.% C (Tutorial 11)
C content [wt.%]
Mn content [wt.%]
Temperature [°C]
Temperature [°C]
Liquid
Liquid
Liquid with BD
Liquid with BD
FCC_A1_S
FCC_A1_S with BD
FCC_A1_S with BD
FCC_A1_S

## Slide 26: Primary precipitates

## Slide 27: Primary precipitates
Primary precipitates  preciptates formed during the presence of the liquid phase
Phases coexistent with the liquid phase at the equilibrium calculation  strong candidates for the primary precipitates
Ni-Cr-Mo-Ti-B-C (0.25 wt.% C)
Equilibrium calculation

## Slide 28: Primary precipitates
Primary precipitates are preciptates formed during the presence of the liquid phase
Phases coexistent with the liquid phase at the equilibrium calculation are strong candidates for the primary precipitates
Ni-Cr-Mo-Ti-B-C (0.1 wt.% C)
Equilibrium calculation

## Slide 29: Primary precipitates
Primary precipitates are preciptates formed during the presence of the liquid phase
Phases coexistent with the liquid phase at the equilibrium calculation are strong candidates for the primary precipitates
Phases appearing close to the liquidus should be also checked
Fe-Nb-Ti-C-N (Example E20)
Equilibrium calculation

## Slide 30: Primary precipitates
Primary precipitates are preciptates formed during the presence of the liquid phase
Phases coexistent with the liquid phase at the equilibrium calculation are strong candidates for the primary precipitates
Phases appearing close to the liquidus should be also checked
Fe-Nb-Ti-C-N (Example E20)
SG-calculation

## Slide 31: Modeling of solid-solid transformation

## Slide 32: Solid-solid transformation
A solid phase might transform to another solid phase
Relevant for the peritectic reaction (e.g. δ-ferrite + liquid  austenite in steels)

## Slide 33: Solid-solid transformation
Transformation type (calculation of the transformed phase ratio)
  Full equilibrium
  Constrained equilibrium
    As „full“, but the back-diffusion constraints are taken into account
  Avrami type
  Koistinen-Marburger
  Manual ratio
    Amounts taken from the table provided by user (Temperature vs. Amount transformed)

## Slide 34: Solid-solid transformation
Transformation type (calculation of the transformed phase ratio)
  Full equilibrium
  Constrained equilibrium
    As „full“, but the back-diffusion constraints are taken into account
  Avrami type
  Koistinen-Marburger
  Manual ratio
    Amounts taken from the table provided by user (Temperature vs. Amount transformed)

## Slide 35: Solid-solid transformation
Technical note
The „From“-phase is taken and transformed to „Equilib phase“-phase (with „_T“-suffix)
„Equilib phase“ might be created with „Create equilib phase…“ from parent phase of the „To“-phase
„_TS“-phase contains all fractions transformed before and at the considered temperature

## Slide 36: Solid-solid transformation
Technical note
The „From“-phase is taken and transformed to „Equilib phase“-phase (with „_T“-suffix)
„Equilib phase“ might be created with „Create equilib phase…“ from parent phase of the „To“-phase
„_TS“-phase contains all fractions transformed before and at the considered temperature
Liquid(CL,1)
BCC_A2
BCC_A2_S
L0  L1 + BCC_A2

## Slide 37: Solid-solid transformation
Technical note
The „From“-phase is taken and transformed to „Equilib phase“-phase (with „_T“-suffix)
„Equilib phase“ might be created with „Create equilib phase…“ from parent phase of the „To“-phase
„_TS“-phase contains all fractions transformed before and at the considered temperature
Liquid(CL,2)
BCC_A2_S
FCC_A1
L1  L2 + FCC_A1

## Slide 38: Solid-solid transformation
Technical note
The „From“-phase is taken and transformed to „Equilib phase“-phase (with „_T“-suffix)
„Equilib phase“ might be created with „Create equilib phase…“ from parent phase of the „To“-phase
„_TS“-phase contains all fractions transformed before and at the considered temperature
Liquid(CL,3)
FCC_A1_TS
BCC_A2_S
FCC_A1
FCC_A1_S
L2  L3 + FCC_A1
BCC_A2_S + L2  FCC_A1_TS

## Slide 39: Solid-solid transformation
Fe-Nb-Ti-C-N (Example E20)
Without peritectic transformation
With peritectic transformation

## Slide 40: Applications

## Slide 41: What do I get from it?
Microsegregation limits obtained:
  Core composition: Composition of the very first „α“-phase appearing
  Intergranular composition: Composition of the liquid phase for a system with some defined liquid content
Cooling | Liquid phase fraction [at. %]
Air-cooling | 1
Continuous casting | 3
Arc furnace | 5

## Slide 42: What do I get from it?
Example: Cu-Ni alloy, 35 wt.% Ni
Temperature [°C]
Ni content [wt.%]
Liquid
FCC_A1_S
FCC_A1
Temperature [°C]
Phase fraction
Liquid
FCC_A1_S
FCC_A1
Core
Intergranular

## Slide 43: What do I get from it?
Primary precipitate characteristics (if present):
  Chemical composition
  Amount (Phase fraction)
Cooling | Liquid phase fraction [at. %]
Air-cooling | 1
Continuous casting | 3
Arc furnace | 5
Above parameters are taken from the system with the liquid phase fraction relevant to the solidification cooling rate

## Slide 44: What do I get from it?
Example: Fe-Nb-Ti-C-N (Example E20)
TiN expected as a primary precipitate
Phase fraction ~1-2*10-5

## Slide 45: Application
Example: Fe-Nb-Ti-C-N (Example E20&P20)
SG-calculation
- Identifying the compositions of solute-enriched and –depleted region
- Identifying the primary precipitates and their amounts
Precipitation kinetics simulation
- Introduction of the precipitate phases representing the primary precipitates
- Simulations performed for both compositions (solute-enriched and –depleted region)

## Slide 46: Acknowledgments
Yao Shan
Georg Stechauner