## Slide 1: Trapping Modelling in MatCalc
Yao V Shan

## Slide 2: Introduction
Trapping: atoms sticking to lattice defects (e.g. solute atoms, dislocations, grain boundaries, …)
Cottrell atmosphere seen as trapping of carbon atoms along dislocations
Pereloma et al. 2007

## Slide 3: Given parameters
Trapping enthalpy ∆E: reduction of system energy per trapped atom
Nominal composition of trapped element ci
Amount of trapping positions cdef (solute atoms: nominal composition of trapping element, dislocations: dislocation density)
Molar volume Ω
Temperature T

## Slide 4: State variables
Concentration of free atoms (in lattice) and trapped atoms: cL cT
Volumes corresponding one mole of lattice positions and trap positions: VL VT
Site fractions in lattice positions and trap positions: yL yT

## Slide 5: Trapping
On solutes:
On dislocations:

## Slide 6: Constraints
Mass balance
Molar volume Ω
Defects generate the molar trapping volume
Site fractions

## Slide 7: Thermodynamics
Gibbs energy:
Effect of trapping
Sc … configurational entropy
ΩcT … moles of trapped atoms
∆E … trapping enthalpy

## Slide 8: Configurational entropy
Bragg-Williams approximation
Dividing the lattice into free and trapped portions:
Ω/VL … fraction of lattice sites
Ω/VT … fraction of trap sites

## Slide 9: Gibbs energy
Gibbs energy
Equilibrium
Applying constraints
Partial derivative

## Slide 10: Gibbs energy derivation
Derivation
Simplifying to
Equilibrium equation
Oriani 1970

## Slide 11: Exact analytical solution
Knowing
and
One can find yL at equilibrium

## Slide 12: Real system
Carbon on dislocations
Trapping enthalpy:
Coordination number Z for dislocations:
Around 15 C atoms on a screw dislocation plane at room temperature (edge dislocation about half as much):
(Clouet et al. 2008)
(Cochardt et al. 1955)
(Cochardt et al. 1955)

## Slide 13: Effect of trapping
Cementite fraction over temperature
Increasing dislocation density dissolves cementite at lower temperatures
Dislocation density

## Slide 14: Expansion to multi elements
Multi trapping: e.g. carbon and nitrogen
Gibbs energy
Equlibrium dG/dyL,C = 0 and dG/dyL,N = 0 leads to
McLean 1957

## Slide 15: Expansion to multi traps
Gibbs energy
Equlibrium equations (i×k equations)
l = 1, 2, …, k
j = 1, 2, …, i

## Slide 16: Kinetics
Kinetics are obtained from the balance equation for the Gibbs energy (thermodynamic extremal principle1):
Total dissipation at dislocations in system due to carbon diffusion
a… acting radius of dislocation
R… radius surrounding dislocation in a unit cell
ρ… dislocation density
D… Diffusion coefficient of carbon
1Svoboda et al. 2006

## Slide 17: Kinetics
At dislocations:
At grain boundaries:
R… grain radius in a unit cell
δ… grain boundary thickness

## Slide 18: Parameter study
Cottrell theory in dashed lines:

## Slide 19: Summary
Thermodynamic model for describing various trapping effects
Derivations of the presented model lead to known equations, which has been used in empirical models for equilibrium
Expansion of model for multi components
Kinetic equations for slow non-equilibrium processes

## Slide 20: More fun…
Chemical potentials
Extracting ∆E from CALPHAD data by comparing chemical potentials
Ruda et al. 2009
Svoboda et al. 2011

## Slide 21: More fun…
Diffusion coefficients
Trapping reduces the effective diffusion coefficient
Svoboda et al. 2011