## Slide 1: MatCalc approach for the modelling of the vacancy concentration evolution (MatCalc 5.60.0005)
P. Warczok

## Slide 2: Outline
Vacancy concentration
  What is it all about?
  Why do we care about?
  How does it evolve?
  Why does it (sometimes) take so long to evolve?

## Slide 3: What is it all about?
Real materials are not perfect crystals...
http://www.tf.uni-kiel.de/matwis/amat/def_en/overview_main.html

## Slide 4: What is it all about?
Equilibrium vacancy concentration  thermodynamics make them appear

## Slide 5: What is it all about?
Equilibrium vacancy concentration  thermodynamics make them appear
Vacancy formation entropies are currently not used in MatCalc
Vacancy formation enthalpies come from thermodynamic database. Feel free to change it, if you need it (Variables& function)

## Slide 6: What is it all about?
Equilibrium vacancy concentration  thermodynamics make them appear

## Slide 7: What is it all about?
Equilibrium vacancy concentration  thermodynamics make them appear

## Slide 8: What is it all about?
Equilibrium vacancy concentration  thermodynamics make them appear

## Slide 9: What is it all about?
How to change the vacancy concentration?
  New equilibrium
    Change temperature
    Transform to a new phase
  Out of equilibrium
    Deform material
    Irradiate material

## Slide 10: Why do we care?
Vacancies
Diffusion
Nucleation
Precipitation kinetics

## Slide 11: Why do we care?
Vacancies
Nucleation
Precipitation kinetics
Chemical part
Elastic part
- Vacancy contribution to driving force
– Gas constant
– Temperature
- Vacancy site fraction on subst. lattice (current)
- Vacancy site fraction on subst. lattice (equil.)
- Critical nucleation energy
– Interfacial energy preciptate/matrix
- Molar volume
– volumetric misfit of precipitate
– Poisson‘s ratio
- Young‘s modulus
– Nucleation rate

## Slide 12: Why do we care?
Vacancies
Nucleation
Precipitation kinetics
Generation/anihilation of the excess vacancies results in a strain of the matrix (last term)
Volumetric misfit of the precipitate may augment/decay the previous effect (second term)
Chemical part
Elastic part

## Slide 13: Why do we care?

## Slide 14: Why do we care?

## Slide 15: Why do we care?
Vacancies
Diffusion
Precipitation kinetics
http://www.doitpoms.ac.uk/tlplib/diffusion/diffusion_mechanism.php
- Diffusion coefficent
- Pre-exponential factor
- Activation energy of subst. diff.

## Slide 16: Why do we care?
Vacancies
Diffusion
Precipitation kinetics
http://www.doitpoms.ac.uk/tlplib/diffusion/diffusion_mechanism.php

## Slide 17: Why do we care?
Vacancies
Diffusion

## Slide 18: How does it evolve?
Sources and sinks
Source
Material
Sink
Equilibrium  Generation rate at source = Anihilation rate at sink
Vacancy flow

## Slide 19: How does it evolve?
3 models in MatCalc:
  Mean diffusion distance
  „FSAK“* model
  Vacancy generation during the deformation (with FSAK only!)
* „Fischer-Svoboda-Appel-Kozeschnik“, Fischer et. al., Acta Mater. 59 (2011) 3463-3472

## Slide 20: How does it evolve?
Mean diffusion distance
  Dislocations are taken as a vacancy source/sink
Default mean diffusion distance:
Evolution equation:
- Mean diffusion distance
– Dislocation density
- Element subst. site fraction
- Constant

## Slide 21: How does it evolve?
Mean diffusion distance
  Dislocations are taken as a vacancy source/sink
Default mean diffusion distance:
Evolution equation:

## Slide 22: How does it evolve?
Mean diffusion distance
  Dislocations are taken as a vacancy source/sink
Default mean diffusion distance
Evolution equation

## Slide 23: How does it evolve?
FSAK: Generation/anihilation on dislocation jogs
Evolution equation:
– Diffusion correlation factor (0.75)
– Burger‘s vector
– Jog density
– Jog fraction on dislocations

## Slide 24: How does it evolve?
FSAK: Generation/anihilation on dislocation jogs
Evolution equation:

## Slide 25: How does it evolve?
FSAK: Generation/anihilation on dislocation jogs
Evolution equation:

## Slide 26: How does it evolve?
FSAK: Generation/anihilation on grain boundaries
Evolution equation:
– Radius of the spherical grain
(0.5 * grain size)

## Slide 27: How does it evolve?
FSAK: Generation/anihilation on grain boundaries
Evolution equation:

## Slide 28: How does it evolve?
FSAK: Generation/anihilation on Frank loops (test-phase?)
Evolution equation:
- Effective loop energy
- Frank loop radius (defined in the console)
- Frank loop density (defined in the console)
- Jog spacing on Frank loops (number of atoms)
- Jog fraction on Frank loops
- Boltzmann constant

## Slide 29: How does it evolve?
FSAK: Generation/anihilation on Frank loops (test-phase?)
Evolution equation:

## Slide 30: How does it evolve?
Vacancy generation during the deformation
Evolution equation:
– Constant
– Taylor factor
– Shear modulus
- Strain rate

## Slide 31: How does it evolve?
Vacancy generation during the deformation
Evolution equation

## Slide 32: Why does it take so long to evolve?
The idea:
  Some vacancies are trapped in the material and do not proceed to the sinks.
  Equilibrium between the trapped an „free-to-move“ vacancies
Needed:
  The amount of traps
  The trapping strength
  Relation between the amounts of trapped and free vacancies

## Slide 33: Why does it take so long to evolve?
Possible traps
  Solute atoms
  Dislocations
  Grain- & subgrain boundaries
  Precipitate surface

## Slide 34: Why does it take so long to evolve?
Possible traps
Trapping site | Fraction of trapping sites
Solute atoms | 
Dislocations | 
Grain boundary | 
Subgrain boundary | 
Precipitate surface | 
Trapping site | Fraction of trapping sites
Solute atoms | 
Dislocations | 
Grain boundary | 
Subgrain boundary | 
Precipitate surface | 
- Number of bulk sites
- Number of sites at grain boundary
- Number of sites at subgrain boundary
- Dislocation core radius (5*10-19 m)
- mole fraction of component „i“
- Number of precipitates in class „j“
- Radius of precipitates in class „j“
- Atomic volume

## Slide 35: Why does it take so long to evolve?
Trap „strength“: delta H
Trap „range“ modifier: coordination number
- Trapping enthalpy

## Slide 36: Why does it take so long to evolve?
The amount of traps
  Amount of lattice sites  expressed by molar volumes
Svoboda J., Fischer F.D., Acta Mater. 60 (2012) 1211-1220
- Total number of lattice sites
- Number of sites on which the vacancy is free to move
- Number of sites on the vacancy traps
- Number of „i“-sites (e.g. )
- Molar volume (volume for = 1)
- Volume of material containing 1 mole of „i“-sites
- Mole fraction of „i“-sites

## Slide 37: Why does it take so long to evolve?
The amount of traps
  Amount of lattice sites  expressed by molar volumes
Svoboda J., Fischer F.D., Acta Mater. 60 (2012) 1211-1220
- Total number of lattice sites
- Number of sites on which the vacancy is free to move
- Number of sites on which the vacancy is trapped
- Number of „i“-sites (e.g. )
- Molar volume (volume for = 1)
- Volume of material containing 1 mole of „i“-sites
- Mole fraction of „i“-sites
For clarity:
is the volume of the material under consideration needed to have the amount of 1 mole of „i“-sites in it. The less „i“-sites in the material, the more of it is needed.
IS NOT the volume of 1 mole of „i“-sites! The material does not consist of „i“-sites alone

## Slide 38: Why does it take so long to evolve?
Vacancy balance
=+
 according fraction of trapping sites*coordination number
 assumed as (molar volume of system)
- Site fraction of vacancies on „i“-sites (= fraction of „i“-sites occupied by the vacancies)
Svoboda J., Fischer F.D., Acta Mater. 60 (2012) 1211-1220

## Slide 39: Why does it take so long to evolve?
Vacancy balance:
Minimization of free energy:
Combine these two above  solve for and
The immobile vacancies 
=+
Svoboda J., Fischer F.D., Acta Mater. 60 (2012) 1211-1220

## Slide 40: Examples
Examples from MatCalc website (P2-1, P2-2)
  FSAK model
  Al-Cu system, 4.3 wt.% Cu
  Precipitates: TH_DP_GPB- (bulk), THETA_PRIME- (disl.), THETA_AL2CU- (disl.)
  Al-fcc domain

## Slide 41: Examples
Al-Cu system (Example P2-1), tempered at 200°C

## Slide 42: Examples
Al-Cu system (Example P2-1), tempered at 150°C

## Slide 43: Examples
Al-Cu system (Example P2-1), tempered at 100°C

## Slide 44: Examples
Al-Cu system (Example P2-1)

## Slide 45: Examples
Al-Cu system (Example P2-2), influence of cooling rate

## Slide 46: Examples
Al-Cu system (Example P2-2), influence of dislocation density

## Slide 47: Examples
System Al-Mg-Si
Mg = 0,4 wt.%, Si = 1,1 wt.%
Mg5Si6_B_DP-precipiate. Nucleates at bulk sites
Al-fcc domain
Trapping sites: Mg (2600 J/mol) and Si (3500 J/mol) solute atoms.
FSAK model

## Slide 48: Examples
Variation of grain size (FSAK)

## Slide 49: Examples
Variation of grain size (FSAK)

## Slide 50: Examples
Variation of trapping enthalpy (FSAK)

## Slide 51: Examples
Variation of trapping enthalpy (FSAK)