## Slide 1: Precipitate shape factors (MatCalc 5.61.0027)
P. Warczok

## Slide 2: Outline
Introduction, definition
  Precipitate growth
  Precipitation strengthening

## Slide 3: Introduction
Usual assumption: spherical precipitates
Matrix contribution
Precipitate contribution
- Gibbs energy of the system
- Number of i moles in the matrix
- Chemical potential of i in the matrix
- Radius of k
- Mechanical contribution of k
- i content in k
- Chemical potential of I in k
- Interfacial energy of k
- element
- matrix
- precipitate class
Precipitate/matrix
interface contribution
Svoboda et. al., Mater. Sci. Eng. A., 385 (2004) 166-174

## Slide 4: Definition
Shape parameter
  Spherical  cylindrical
  Cylinder aspect ratio
- Shape parameter
- Cylinder height
- Cylinder diameter
Needles
(prolate)
Discs
(oblate)
Kozeschnik et. al., Mater. Sci. Eng. A., 441 (2006) 68-72

## Slide 5: Definition

## Slide 6: Effects
Shape modification  interface area changed
For h = 1  Sk = 1.1447 !
Kozeschnik et. al., Mater. Sci. Eng. A., 441 (2006) 68-72

## Slide 7: Effects
Influence on Gibbs energy dissipation contributions Q
Matrix
diffusion
Precipitate
diffusion
Interface migration
Kozeschnik et. al., Mater. Sci. Eng. A., 441 (2006) 68-72

## Slide 8: Precipitate growth
Evolution equations affected

## Slide 9: Precipitate growth

## Slide 10: Precipitate growth

## Slide 11: Precipitate growth
Shape factors do not influence the precipitate nucleation stage in MatCalc !!!

## Slide 12: Precipitate growth
Growth rates
(Anisotropy effects neglected!)
Minimal diffusion distances for disc growth
Kozeschnik et. al., Mater. Sci. Eng. A., 441 (2006) 68-72

## Slide 13: Precipitation strengthening
Surface-surface precipitate distance
Shear stress
Shear stress for Orowan mechanism
Shear stress for shearable precipitates
Distance between the precipitates
Precipitate radius
Outer cut-off radius
Equivalent radius
Sonderegger B., Kozeschnik E., Scripta Mater., 66 (2012) 52-55

## Slide 14: Precipitation strengthening
Surface-surface precipitate distance
Shear stress
Distance between the precipitates
Distance between the spherical precipitates
Sonderegger B., Kozeschnik E., Scripta Mater., 66 (2012) 52-55

## Slide 15: Precipitation strengthening
Equivalent radius - Shearable precipitate
Equivalent radius for edge disl.
Sphere radius for edge disl.
Equivalent radius for screw disl.
Sphere radius for screw disl.
Fraction of edge disl.
Fraction of screw disl.
Ahmadi M.R. et al., Mater. Sci. Eng. A, 590 (2014) 262-266

## Slide 16: Precipitation strengthening
Equivalent radius - Shearable precipitate
Ahmadi M.R. et al., Mater. Sci. Eng. A, 590 (2014) 262-266

## Slide 17: Precipitation strengthening
Outer cut-off radius – Orowan mechanism
Equivalent radius for edge disl.
Sphere radius for edge disl.
Equivalent radius for screw disl.
Sphere radius for screw disl.
Fraction of edge disl.
Fraction of screw disl.
Ahmadi M.R. et al., Mater. Sci. Eng. A, 590 (2014) 262-266

## Slide 18: Precipitation strengthening
Outer cut-off radius – Orowan mechanism
Ahmadi M.R. et al., Mater. Sci. Eng. A, 590 (2014) 262-266

## Slide 19: Precipitation strengthening
Dislocation characterization